## Slide 1: Polarimetric Components for UV Space Instrumentation
Silvano Fineschi
INAF-Torino Astrophysical Observatory, Italy
Juan Larruquert,
CSIC Madrid, Spain
Marco Malvezzi
Univ. Pavia, Italy

## Slide 2: Coronal Magnetism

## Slide 3
Blos
UV (permitted) lines: Blos ;los
VIR (forbidden) lines: pos
solar/stellar atmosph.

## Slide 4: Hanle Effect (tutorial)
Larmour  A

## Slide 5
A [107 s-1] ~ 0.88  gJ  B [G]
Hanle effect Sensitivity

## Slide 6: Hanle effect in Stellar Atmospheres
Ignace et. Al. 1999

## Slide 7
(Min. Detectable Rot. Angle)  ~ P/P

P
P
P (Min. detectable Polariz.) ~ 1/signal-to-noise ratio  1/ Troughput
P  P0  (T// -T)/(T// +T)  P0  
 [rad] ~ P0 / (   Troughput)
Figure-of-merit,      Troughput

## Slide 8: Brewster-angle UV Polarizers (metals)
Low Polarization
High Througput
 =0.3

## Slide 9: Brewster-angle UV Polarizers (Alkaline crystals)
High Polarization
Low Througput
 =0.4

## Slide 10: Brewster-angle UV Polarizers

## Slide 11: VUV Brewster-angle polarizers
Windows LiF / MgF2 @ Brewster-angle
s
s + p
3-reflection polarizer
polarization m = 95%
trasnsmission: ≈ 15%
Figure-of-merit = 0.37
Pros: On optical axis
Cons: Critical alignment
Image rotation
LiF: Rs = 0.205
m = 1, k = 0.32
S
P
MgF2: Rs = 0.335
m=1, k = 0.41
S
P
Figure-of-merit: k=(S-P)/(2(S+P))1/2=
=m R1/2, 0 ≤ k ≤ 2-1/2
polarization m=(S-P)/(S+P)
0 ≤ m ≤ 1

## Slide 12: Thin-film Coatings for UV polarizers I: design
“transparent”materials: LiF, MgF2
“absorbing” materials: metals Al, Au, Pt ...
strategy:
induced trasmission/reflection (Berning & Turner, JOSA 1957)
Optical constants of VUV film coatings are (somewhat) different from those of bulk substrates
F.Bridou et al, Opt Comm. 283, 1351 (2010)

## Slide 13: Thin-film Coatings VUV polarizers II : simulations
121.6 nm, 45°
121.6 nm, 45°
RS
Rave
m
k
RP
RS
m
k
RP
MgF2/Al
RS
Rave
m
k
RP
RS
m
k
RP

## Slide 14: Thin-film Coatings for VUV polarizers III: Measurements (BEAR facility at Synchrotron Trieste, Italy)
65° 60°
Rp
. Feb 2013
_ Oct 2013
Ly a
Ly a
65° 60°
. Feb 2013
_ Oct 2013
Rp
Rs
65° 60°
Ly a
MgF2 and metals on glass substrate (CSIC Madrid)
Anle-of-incidence: 60°
Stability issues (in air storage)
= 0.99   0.35 = 0.6

## Slide 15: Thin-film Coatings for VUV polarizers IV: Measurements (BEAR facility at Synchrotron Trieste, Italy)

## Slide 16: Transmission VUV Polarizers
Thin-film coatings for transmission polarizers :
No image rotation
Intrinsic narrow.band capability
Brewster-angle reflection:
Brewster-angle transmission:

## Slide 17: Thin-film for Transmissive VUV Polarizers
TS
TP
TP
TS
Feb ‘13
Oct ‘13
Feb ‘13

## Slide 18
Thin-film Coarings for Transmissive VUV Polarizers II
Angle-of-incidence
q = 12°
Max Transmission P :
TP = 0.16 a 124 nm e q = 28°
Min. Transmission S:
TP< 0.01 a q ≈12°
at  = 121.6 nm:
= 0.24
TP(l,q)
TS(l,q)
m(l,q)
k(l,q)

## Slide 19: Thin-film Coarings for Transmissive VUV Polarizers III
Transmitting polarizer
Interference filter (Pelham Ltd):
Band-pass transmitting polarizer = 0.24
vs.
Triple-reflection polarizer (= 0.37)
with band-pass filter (T=0.18) => = 0.16

## Slide 20: Piezo-Birefringence I
Pressure constants
Pressure along 001
Phase change induced by LiF
Elettra
LiF
Analyzer
Detector

## Slide 21: Piezo-Birefringence II
calibrazione del carico sul cristallo
calibrazione del ritardo ottico nel visibile
formalismo dei vettori di Stokes e matrici di Mueller
ingresso non polarizzato: {1,0,0,0}
uscita = T(j) . Mlph . T(-j). T(-45).Rhor(x). T(45).Mlph.{1,0,0,0}
T: rotazione
Mlph: polarizzatore lineare orizzontale
Rhor: ritardo ottico con asse veloce orizzontale
Q11 – Q12 |exp =6.15 10-12 m2 N-1
a ≈ 600 nm:
con P = 3 MPa si ottiene una
rotazione di 17° a 600 nm. (c’è ancora un fattore 3 per raggiungere il carico critico)
NB:
Q11 – Q12 |120nm=33 10-12 m2 N-1
Sanchez & Cardona phys. stat.
sol. (b) 50, 293 (1972)

## Slide 22: Cryo-Piezo-Birefringence
Ly b
300 K
77K